Supporting Information

Table S1. Semiochemical release system. Release rates of hexanal and benzaldehyde from polyethylene vials (0.9mm-thick walls) as the % of product remaining after 0 to 20 days and with varying initial loads (50, 100, and 200μl) and temperatures (20 or 27°C) [S1]. In the field trials, heat-sealed polyethylene sachets with 0.1mm-thick walls and loaded with either 200 or 500μl of semiochemicals were used instead of the more costly vials

| Days | Hexanal | Benzaldehyde |
| --- | --- | --- |
|  | 50μl | 100μl | 200μl | 50μl | 100μl | 200μl |
|  | 20°C | 27°C | 20°C | 27°C | 20°C | 27°C | 20°C | 27°C | 20°C | 27°C | 20°C | 27°C |
| 0 | 100 | 100 | 100 | 100 | 100 | 100 | 100 | 100 | 100 | 100 | 100 | 100 |
| 2 | 98.0 | 95.9 | 99.1 | 97.7 | 100 | 98.9 | 100 | 98.5 | 99.8 | 99.1 | 100 | 99.0 |
| 6 | 88.2 | 79.8 | 93.3 | 87.7 | 96.6 | 93.8 | 100 | 87.1 | 98.0 | 94.1 | 100 | 94.9 |
| 9 | 82.7 | 69.8 | 88.0 | 80.1 | 93.4 | 89.4 | 97.4 | 79.3 | 96.3 | 89.8 | 99.2 | 92.1 |
| 15 | 66.6 | 54.8 | 78.0 | 66.4 | 87.2 | 81.1 | 89.8 | 58.1 | 89.9 | 80.5 | 95.7 | 86.3 |
| 20 | 59.2 | 49.8 | 71.2 | 59.3 | 81.9 | 75.1 | 83.7 | 53.6 | 85.1 | 73.5 | 91.5 | 81.9 |

Reference

S1. Cork A, Zerba E, Camps Diez F, Rojas de Arias A. Development of an odour-baited trapping system for control of the vector of Chagas disease, Triatoma infestans. First and Second Annual Reports. Inco DC: International Cooperation with Developing Countries (1994-1998). Contract number ERB18*CT980356.