Table S1. Constants and correlation coefficients of Pb(II) and Cd(II) adsorption by langmuir and Freundlich model

| Model | Pb(II) | Cd(II) |
| --- | --- | --- |
|  | Constants | R2 Constants | R2 |
| Langmuir | qmax=333.33 (mg g-1) | b = 0.12 (L mg-1) | 0.994 | qmax=166.67 (mg g-1) | b = 0.025 (L mg-1) | 0.996 |
| Freundlich | kf =99.7 | 1/n = 0.62 | 0.974 | kf = 13.80 | 1/n=0.461 | 0.984 |