Table S2

Average droplet diameter and PDI of nanoemulsions A and B before and after incubation in media.

| Media incubation | Nanoemulsion A | Nanoemulsion B |
| --- | --- | --- |
|  | Average diameter (nm) | PDI | Average diameter (nm) | PDI |
| Before | 144.6 | 0.113 | 123.8 | 0.156 |
| After | 140.6 | 0.135 | 128.7 | 0.149 |