Supplemental Information

Table A: Water contents in hydrated PMEA-analogous polymers (wt%) [1]

Supplemental Table 1: Water contents in hydrated PMEA-analogous polymers (wt%) [21]

| Description | PBA | PTHFA | PMEA | PMe3A | PMe2A | PMPC |
| --- | --- | --- | --- | --- | --- | --- |
| Bound water | 0.68 | 4.1 | 6.3 | 42 | 36 | 55 |
| Intermediate water | 0 | 1.3 | 3.8 | 20 | 21 | 29 |
| Non-freezing water | 0.68 | 2.8 | 2.5 | 22 | 15 | 26 |

The content of water in the homopolymers of 2-(2-methoxyethoxy) ethoxy ethyl acrylate, 2-methacryloyloxyethyl phosphorylcholine, and 2-methacryloyloxyethyl phosphorylcholine are shown as the contents of water in hydrated PMe3A, PMe2A, and PMPC, respectively.

Figure A

Focal adhesion formation of MDA-MB-231 on PMEA-analogous polymer substrates after 1 day. Blue, green, and red colors depict cell nuclei, actin filaments, and vinculin, respectively. The white arrow head indicates a focal adhesion. The bar indicates 10 m.

Figure B

Focal adhesion formation of HepG2 on the PMEA-analogous polymer substrates after 1 day. Blue, green, and red colors depict cell nuclei, actin filaments, and vinculin, respectively. The white arrowhead indicates a focal adhesion. The bar indicates 10 m.

Figure C

Relationship between intermediate water content and protein adsorption. (A) Relationship between intermediate water content and the amounts of adsorbed FBS proteins. The data represent the means ± SD (n=5). (B) Relationship between intermediate water content and exposed cell attachment site in FN. The data represent the means ± SD (n=4).

Figure D

Relationship between intermediate water contents and cell attachment after incubation for (A) 30 min, (B) 60 min, and (C) 180 min. The square and circle plots indicate HT-1080 and HepG2, respectively. The shadowed window indicates intermediate water contents that showed high HT-1080 attachment and low HepG2 attachment.

Figure E

Chemical structure of PMEA analogous polymers.