**S9 Table: Tape lift sheddability data for the tested garments.** The table shows the number of fibers counted within 1 cm2 windows tape-lifted from the 100% Cotton and 100% Polyester T-shirts used in the testing.

|  |  |  |
| --- | --- | --- |
|  | **Fibers Counted on Selected Window/ cm2** | |
| **Selected Window** | **Red Cotton T-shirt** | **Black Polyester Jersy** |
| Tape lift 1 | 4 | 2 |
| Tape lift 2 | 10 | 0 |
| Tape lift 3 | 25 | 0 |
| Tape lift 4 | 26 | 1 |
| Tape lift 5 | 17 | 1 |
| Tape lift 6 | 25 | 1 |
| **Average** | **17.8** | **0.83** |
| **Standard Deviation** | **9.20** | **0.75** |