Supplementary Information

Sublethal effects of CuO nanoparticles on Mozambique tilapia (Oreochromis mossambicus) are modulated by environmental salinity

Fernando Villarreal1*¶, Gautom Kumar Das2¶, Aamir Abid2, Ian M. Kennedy2 and Dietmar Kültz1

¶ Authors contributed equally to this work

1Physiological Genomics Group, Department of Animal Science, University of California-Davis

2Department of Mechanical and Aerospace Engineering, University of California, Davis, CA 95616, USA

* Corresponding author

e-mail: fvillarreal@ucdavis.edu

Figure S1. Schematic of flame generated NP synthesis system and collection in a baghouse filter.

Figure S2. XRD pattern of the CuO NP. (A) XRD of the as-synthesized NP (B) XRD of the CuO powder samples probe sonicated for 5 min with a 20 s sonication followed by 10 s rest. Both the patterns are identical suggesting no change in physicochemical properties due to sonication.

Figure S3. The Zeta Potential of the NP dispersion in fresh water fish tanks at different time points (from top to bottom, Day 0 to Day 8).