| Table S2. Phase transition temperatures for glycosides in an anhydrous condition from literatures. The lamellar distance of bilayers, d (in Å). |
| --- |
| Lipid | Symbol | d-spacing/ Å | Pre-transition temp | Solid–L( | L(–iso. | Ref |
|  |  | ( at 20°C) | (°C) | transition temp | transition temp. |  |
|  |  |  |  | (°C) | (°C) |  |
|  |  |  |  |  |  |  | (d-spacing) |  |  |
| Octyl β-glucoside | βC8Glu |  |  |  |  |  | 69.0 | 107.0 | [10] |
| Octyl β-maltoside | βC8Mal |  |  |  |  |  |  | 122.7 | [52] |
| Decyl β-maltoside | βC10Mal |  |  |  | 78.6(c) |  | 96.5 | 203.0 | [52] |
| Decyl β-maltoside | βC10Mal |  |  |  |  |  | 38.6 | 102.2 | [52] |
| Decyl β-maltoside | βC10Mal |  | 25(a) | 25(b) |  |  |  | 208.0 | [52] |
| Dodecyl β-maltoside | βC12Mal | 33.5 |  |  | 70(c) |  | 103.0 (41.5 Å) |  | [19] |
| Dodecyl α-maltoside | αC12Mal | 33.5 |  |  | 50(c) |  | 128.0 ( 32.4 Å) |  | [19] |
| Tetradecyl β-maltoside | βC14Mal |  |  |  |  | 95(d) | 105.0 (40-41 Å) | 263.0 | [18] |
| Hexadecyl β-maltoside | βC16Mal |  |  |  |  |  | 105.0 |  | [18] |
| Note: (a) glassy state before heating (b) glassy state after heating (c) solid/solid transition (d) not solid/solid transition. |