S1 Table Magnitude of membrane leakage from bacterial cells after exposure to silver nanoparticles.

| Bacteria | Protein content (µg ml-1) | Carbohydrate content (µg ml-1) | Nucleic acid content (µg ml-1) |
| --- | --- | --- | --- |
|  | Control | Protein-capped silver nanoparticles | Bare silver nanoparticles | Control | Protein-capped silver nanoparticles | Bare silver nanoparticles | Control | Protein-capped silver nanoparticles | Bare silver nanoparticles |
| Gram positive |  |  |  |  |  |  |  |  |  |
| B. cereus | 3.99 ± 0.1 | 99.54 ± 9.4 | 108.33 ± 14.7 | 2.19 ± 0.5 | 88.13 ± 3.5 | 97.28 ± 6.3 | 0.98 ± 0.09 | 7.74 ± 0.5 | 9.43 ± 0.6 |
| S. aureus | 4.78 ± 0.1 | 88.34 ± 14.9 | 94.86 ± 9.6 | 6.42 ± 1.0 | 93.86 ± 5.3 | 105.47 ± 9.9 | 0.75 ± 0.13 | 8.73 ± 0.4 | 8.92 ± 0.3 |
| Gram negative |  |  |  |  |  |  |  |  |  |
| E. coli | 8.33 ± 0.6 | 134.38 ± 9. 6 | 154.72 ± 12.2 | 6.28 ± 1.3 | 128.41 ± 9.9 | 144.49 ± 5.4 | 0.35 ± 0.07 | 10.45 ± 0.2 | 11.73 ± 0.7 |
| P. putida | 6.54 ± 0.3 | 105.85 ± 6.5 | 129.26 ± 14.3 | 3.57 ± 0.8 | 113.37 ± 8.1 | 128.46 ± 9.8 | 0.57 ± 0.19 | 10.72 ± 0.4 | 14.37 ± 0.2 |

± represents standard error (n = 3)