S1 Appendix

Curdlan interaction with aniline blue dye

Solutions of the following concentrations of pre-gelled commercial curdlan and of curdlan produced by Agrobacterium sp. IFO 13140 (pre-gellation method) were prepared in NaOH 5 mmol L-1: 0, 50, 100 and 150 µg mL-1. These solutions were mixed with an equal volume of phosphate buffer (0.5 mol L-1, pH 7) containing 160 mg L-1 of aniline blue and kept for 120 min at room temperature. Then, the absorbance of the mixtures was measured at 590 nm. The analysis was performed in triplicate.

Fig S1. Relationship between absorbance difference and concentration of curdlans. Pre-gelled commercial curdlan (●) and curdlan produced by Agrobacterium sp. IFO 13140 recovered by the pre-gellation method (□).